## Slide 1
An Overview of Kinetic Inductance Detectors and Applications
Simon Doyle – Cardiff University

## Slide 2: Talk Overview
Motivation for technology development
Basic introduction to superconductor below the transition temperature
The concept of Kinetic Inductance
Basics description of superconductors at RF frequencies.
Basic operating principal of a Kinetic Inductance Detector
Resonator types and differences
Multiplexed readout electronics
Current and future KID based instruments

## Slide 3: Motivation for detector development - Astronomy
Semi-conductor technology Limited to wavelengths of order 200um (1.5 THz)
Heterodyne receivers are typically noisy and not practical for large format imaging arrays
Bolometers have sensitivity but poor multiplexing ratios
Semi- conductor technology

## Slide 4
Motivation for detector development – Security and Industry

## Slide 5: Motivation for detector development - Astronomy
Pixel counts in Astronomical receivers over the years

## Slide 6: Basic Principals of a Superconductor
Superconductors are most famous for demonstrating zero DC resistance at temperatures below the transition temperature (TC)
It would seem that the Physical properties of the superconductor is not changing below Tc. However ……..

## Slide 7: Below The Transition Temperature
Below Tc the electron population is dividing into separate populations.
A population of electrons weakly bound together called Copper pairs, bound together with an energy 2Δ (typically 0.4 meV) and denoted as ns.
The remaining normal state electrons denoted nn or nqp
The populations can be described to first order by -
nn Behave as normal state electrons.
ns Are paired electrons bound by and Energy 2Δ. These paired electrons are immune from scattering and hence loss

## Slide 8: The conductivity of normal metals (Drude model)
τ is typically of order 10-14 s and at practical frequencies, say f=5GHz (ω=3x1010) leaving ω2τ2 << 1 and the imaginary term negligible.
m = 9.1x10-31
nn ≈ 1029

## Slide 9: Conductivity of non-scattering electrons
The phenomena of superconductivity arises from the non-scattering properties of the superconducting electron population ns.
Consider the Drude model where τ  ∞ to denote a non-scattering electron population ns.

## Slide 10: What is Kinetic Inductance?
A complex surface impedance associated with the inertia of a non-scattering electron population in a superconductor (Cooper-pairs).
As an electron is accelerated in an electric field it gains kinetic energy due to the velocity gained and the electron mass.
When the field is reversed the kinetic energy gained must be returned to the field before the electron can change direction. The electron velocity is proportional to the current, hence the current will lag the field as it would in an inductor.

## Slide 11: The two fluid model of superconductors
The resistive behavior of a superconductor at RF frequencies can be explained by considering the two fluid model.

## Slide 12: Quasi-particle lifetime
A Cooper pair can be split, by say absorbing a photon of energy hf>2Δ. The time for the quasi-particle to recombine to form a Cooper pair is dictated by the quasi-particle lifetime given by Kaplan theory:
Here τ0 is a material dependent property
P.J. de Visser, et al., J. Low Temp. Phys., vol. 167, no. 3–4, pp. 335–340, Jan. 2012.

## Slide 13: Response to change in quasi-particle density
Change in Lint with temperature is small at T << TC
Change in Lint with quasi-particle number typically of order 10-18 H/QP
30nm Al film 4x4μm patch simulated over 200-500mK

## Slide 14: To recap
Superconductor have two electron population
  A normal state population giving a conductivity σ1
  A paired population that does not scatter giving a conductivity σ2
  Photon absorption alters the populations increasing σ1 and reducing σ2.
  The number of quasi-particles generated for a given power is proportional to the quasi-particle lifetime.
  This is the basis of photon detection

## Slide 15: How to measure small changes in surface impedance
Change in internal inductance is still relatively small for typical variations in source power
This small change can be sensed using:
  Hi Q microwave resonators
  Low noise cryogenic amplifiers

## Slide 16: Basic principals of a Kinetic Inductance Detector

## Slide 17: Types of KID detector – The Lumped Element Kinetic Inductance Detector (LEKID)

## Slide 18: Types of KID detector – Distributed Kinetic Inductance Detector (MKID)

## Slide 19: Measuring the sensitivity
The sensitivity of any detector is measured by:
  Measuring the response to optical power – in the case of the KID dF0/dP.
The sensitivity then depends on how accurately you can measure this response. We define a time over which we average measurement of the response to be 0.5s.
  For a KID we measure F0 for 0.5s and establish an error in our measurement. This is the noise

## Slide 20: Measuring the sensitivity
Noise occurs over a range of frequencies and forms a noise spectrum.
In practice me measure this noise spectrum.
This is done by measuring F0 for a period of time and taking a Fourier transform.
The resulting Fourier transform is scaled to give the noise in a 1 Hz bandwidth (0.5s) of integration as a function of frequency.

## Slide 21: KID readout in the complex plane (IQ)
Tone in
Tone out

## Slide 22: Measuring sensitivity
Detector

## Slide 23: Response to photon absorption

## Slide 24: Typical noise spectra of a KID
Roll off due to Quasi-particle lifetime
Amplifier noise floor
Inherent detector noise
GR or Photon
Generally clean noise spectra due to low susceptibility to EM noise sources.
100
101
10-1
10-2
100
101
103
102
104
105
Frequency noise [Hz2/Hz]
Frequency [Hz]

## Slide 25: So we have a sensitive detector!
KID detectors are extremely sensitive.
Reach the photon noise limit down to powers of 1fW (10-15W)
This is the limit of any measurement imposed by the natural noise associated with the random arrival rate of photons from a source.
KID at 220mK
KID at 100mK better performance from cooling further

## Slide 26: Putting NEP into context
A 100W incandescent light bulb produces about 5W of optical power.
If we placed our detector on a modest telescope with 1m2 collecting area, how far away can our light bulb be an still be detected in 0.5 second of observing?
NEP=5x10-18 W/s0.5 which means we have a signal to noise ratio of 1 if we observe for 0.5s. If we observe for 1 second this increases by √2 ≈ 1.4 - so just observable.
Flux at distance D from bulb
We collect over the 1m2 area of the telescope so:
About 70% of the distance to the moon!

## Slide 27: Natural multiplexing in KID devices
Each LEKID is a high Q micro-resonator with a tunable f0
We can therefore multiplex many LEKIDs onto a single CPW feed-line

## Slide 28: Principal of operation - Multiplexing

## Slide 29: Simple Readout Electronics
Warm
Cold
Tone Generation
Mix up / Down
Probe KID
Light in through optics. E= hυ >2Δ

## Slide 30: Making an array of LEKIDs
In most cases 1 deposition and etch step
Minimal material costs
Cleanroom time ½ day

## Slide 31: Optical coupling and band defining

## Slide 32: Current Instruments NIKA on IRAM
NIKA A dual band (150GHz and 220 GHz) mm astronomical camera on the IRAM telescope working just above the photon noise limit at 2mm
M87
1000 pixels @ 2mm
2 x 4000 pixels @ 1mm (2 arrays polarisation sensitive).

## Slide 33: KIDcam – A Terrestrial THz imager

## Slide 34: KIDcam – A Terrestrial THz imager

## Slide 35: On-Chip Spectrometers
High TC material like Niobium
hν<2Δ νcut ≈ 600 GHz
Low TC material like Aluminium
Hν>2Δ νcut ≈ 90 GHz

## Slide 36
On-Chip Spectrometer Results

## Slide 37: Current applications – Optical photon counting and energy resolving detection
Images courtesy of Ben Mazin, University of Santa Barbara, USA

## Slide 38: Conclusion
Relatively immune to temperature fluctuations
Very easy to fabricate (single layer process)
Inherently easy to multiplex – MUX ratios of up to 10’000 are achievable
Are sensitive – will meet the photon-noise limit in most cases
Can be used to energy resolve for single photon counting applications.
Are fast – time constants typically of order 10-50 microseconds
LEKIDs have been demonstrated to work across a wide range of sensing applications. Some of the key benefits of LEKIDs are:

## Slide 39: Two-Fluid model of a Superconductor
Below Tc, the electron population splits into two separate population
  One of normal electrons known as Quasi-Particles
  One of electrons paired together with a typical binding energy 2Δ of around 0.4 meV (Aluminium). These paired electrons are commonly known as Cooper pairs.
The quasi-particle population acts as a normal metal would do, i.e. is resistive. This gives us a conductance σ1
The paired population are have no resistance but do have an associated reactance known as Kinetic Inductance / Internal Inductance. This gives us a conductance jσ2
Absorption of a photon with hυ> 2Δ breaks Copper pairs and alters these populations.

## Slide 40: Internal Inductance for practical film thicknesses
Quite often we are working between the limits of t << L and t >> L. In this case we need to perform the surface integrals for current over the entire ﬁlm cross-sectional area and take into account any variations in current density.

## Slide 41: The London penetration depth
For a non-scattering electron volume
For a superconducting electron volume
Applying Maxwell’s equations to a perfect conductor displays diamagnitism of AC magnetic fields.
London and London suggested a set of constitutive conditions to Maxwell’s equations so that both DC and AC fields as expelled from the bulk of a superconductor.
The field decays to 1/e of its value at the surface within the London penetration depth λL.
The London Penetration depth

## Slide 42: Is a commercial sub-K system viable?
Modern pulse tube systems now cryogen free and push button operation.
Closed cycle systems can be automated and continuous. No user input necessary.